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	Product name
	Antimony Trichloride

	Synonyms
	Antimony(III) chloride; antimonous chloride; butter of antimony

	Molecular formula / weight
	SbCl3 / 228.12 g/mol

	Source basis
	YXL product test report: batch AT20250312; production and test date March 12, 2025

	Specification standard
	HG/T 3464-2014

	Typical HS classification
	2827.39 / 2827.39.90, subject to buyer's destination-country customs ruling


Product Description
YXL Antimony Trichloride is a high-purity inorganic antimony chloride supplied for industrial and technical applications requiring controlled SbCl3 assay and low metallic impurities. The material is moisture-sensitive and should be handled under dry conditions.
Technical Specification
The following specification is transcribed from the YXL product test report shown in the supplied image. Typical result refers to batch AT20250312.
	Test item
	Unit
	Specification
	Typical result

	Antimony trichloride (SbCl3)
	%
	>= 99.9
	99.90

	Antimony (Sb)
	%
	>= 53
	53.01

	Sodium (Na)
	%
	<= 0.02
	0.017

	Potassium (K)
	%
	<= 0.01
	0.0088

	Iron (Fe)
	%
	<= 0.002
	0.0018

	Copper (Cu)
	%
	<= 0.001
	0.001

	Arsenic (As)
	%
	<= 0.005
	0.002

	Lead (Pb)
	%
	<= 0.005
	0.0025

	Hydrochloric acid insoluble matter
	%
	<= 0.005
	0.0025

	Sulfate
	%
	<= 0.08
	0.07


Physical and Chemical Information
	Appearance
	White to colorless crystalline solid; hygroscopic

	Melting point
	Approx. 73.4 deg C

	Boiling point
	Approx. 223 deg C

	Density
	Approx. 3.14 g/cm3

	Water reaction
	Hydrolyzes in the presence of moisture/water; protect from humidity


Applications
	Use areas
	Industrial chemical intermediate; antimony source for specialty formulations; catalyst/reagent applications where SbCl3 is specified

	Customer support
	Sample evaluation and formulation discussion are available through YXL technical sales


Packaging, Storage and Handling
	Packaging
	Sealed, moisture-protective packaging; UN-approved packaging required where regulated for transport. Final pack size per sales confirmation.

	Storage
	Store tightly closed in a dry, cool, well-ventilated area. Protect from moisture and incompatible materials.

	Handling
	Use appropriate PPE and local exhaust ventilation. Avoid dust, contact with skin/eyes, and exposure to moisture.

	Shelf life
	Confirm by batch COA and storage conditions.


Transport and Safety Note
	UN number
	UN 1733

	Proper shipping name
	Antimony trichloride, solid

	Hazard class / packing group
	Class 8 / Packing Group II

	Safety / disclaimer
	This TDS is not an SDS. Review the current YXL SDS and local regulations before storage, handling, disposal, or transport. The information is provided in good faith for product identification and preliminary technical evaluation, and does not constitute a warranty or substitute for buyer qualification, regulatory review, or application testing.
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